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Facility:		Rassau Recycling Facility		Form Number: 	Performance1 / 15/04/2014

Reporting of other performance indicators for the period 01/01/2019 to 31/12/2019

	Parameter
	
	Units 
	

	
	
	
	

	Total raw material used 
	 62,841 tonnes annually *
	

	Battery recycling efficiencies
	96%  Annually
	

	Total amount of raw material  received on site
	62,841 tonnes **
	

	Amount of raw material sent for smelting & refining 
	75,877 tonnes***
	

	Screened material sent for off-site disposal
	 2,830.45 tonnes ****
	



	Operator’s comments :
*Total raw materials used includes all deliveries of Lead bearing materials to site, including whole batteries.
 ** This is the same figure as detailed under *.
 ***This includes all lead bearing materials  etc. 
**** This is furnace slag
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Signed 	Date   30th  January 2020   	
	

(Authorised to sign as representative of Operator)
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