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Phoenix Wood Chip Specification
Phoenix Wood Chip is produced from “Grade A” Pallet wood and conforms to the specification outlined below
	Parameter
	

	Size
	G30

	Feedstock source
	· Grade A recycled pallet wood

· Free from wood preservatives

· Meets the sustainability requirements of  EN14961-2

	Net Calorific Value  (MJ/Kg)
	16.0<

	Moisture
	Typically 10%<15%(average)<25%

	Ash content
	Average <1.5% (maximum 3%)

	Ash Fusion temperature(Deformation) Degree C
	1200 <

	Chemical Composition
	Meets the requirements of EN1961-2 for the production of ENB Wood pellets

	Associated Accreditations
	· BSL0118902-0002 (Chip)

· BSL0118902-0001 (Pellets)

· ENA2 (awaiting accreditation number from HETAS)

· ENB(awaiting accreditation number from HETAS)
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